Study of Dimensional Stability in FDM-Based 3D Printing for Waste Segregation and Elimination Using Intelligent Machine Components

Author(s): Atish Kumar Halder1, Ayush Kumar Singh2, Kunal Bhattacharjee3, Rohit Singh4, Assistant Professor Anish Deb5, Prosenjit Saha6, Sudeb Kundu7, Sanjay Kumar Vishwakarma8, Sanbit Sundar Mondal9. 
Affiliation: Department of Mechanical Engineering, Asansol Engineering College, Asansol, West Bengal, India

Abstract—This paper investigates the dimensional stability of Fused Deposition Modelling (FDM) 3D printed components made from recycled plastic waste materials, specifically in the context of intelligent waste segregation and elimination systems. The inclusion of artificial intelligence (AI) and machine learning (ML) components in such systems is intended to improve the efficiency of automated sorting and processing. The experimental investigation is concerned with process capability, mechanical strength, and dimensional stability of printed components under different conditions. The findings of this research suggest that recycled materials can provide similar dimensional stability to virgin materials when optimized, potentially reducing the environmental impact of recycling. A framework for sustainable production of intelligent waste management devices is proposed.

Key Terms -FDM 3D printing, dimensional stability, recycled waste materials, intelligent waste segregation, AI-integrated machines, sustainable manufacturing

INTRODUCTION

The recent growth in additive manufacturing, particularly Fused Deposition Modelling (FDM), has brought about a revolution in prototyping and manufacturing in various industries. However, the issue of material wastage and environmental sustainability remains a challenge. The focus of this research is on the dimensional stability of FDM-printed parts made from recycled plastic waste, designed for use in intelligent waste segregation and disposal systems. These systems consist of AI-integrated components for real-time sorting, monitoring, and optimization, thus minimizing human interaction and maximizing efficiency.

Waste segregation involves the separation of various materials like plastics, metals, glass, and paper, often done automatically using smart bins and robotic separators. The addition of “live” intelligent components like AI-enabled sensors and actuators to these systems enables dynamic adjustment according to waste flow. Using recycled filaments in FDM printing for such components promotes a circular economy by encouraging the reduced use of raw materials and reducing landfill waste. The primary aim is to evaluate the effect of recycling on the dimensional stability of printed components, which is the ability of printed objects to maintain their desired geometries after printing without warping or shrinking. This is particularly important for functional parts in waste management machines, which require strict tolerances for efficient functionality.

METHODOLOGY

A. Material Preparation

Recycled polyethylene terephthalate (rPET) from plastic bottles was chosen due to its recyclability and ease of access. The bottles were washed, reduced to flakes, dried at 65-70°C, and then extruded into filaments with a diameter of 1.75 mm using a specially designed apparatus. Virgin polylactic acid (PLA) was used as the control material.

B. Additive Manufacturing Setup

An FDM (fused deposition modelling) printer, represented by the Raise3D Pro3, was used. The printing conditions were as follows: nozzle temperature of 200-220°C, bed temperature of 60°C, layer thickness of 0.2 mm, and printing speed of 50-80 mm/s. Test samples included standard ASTM D638 tensile specimens and custom parts like sensor modules for waste sorting.

C. Integration of Intelligent Components

Printed parts included pre-designed slots for artificial intelligence modules (such as a Raspberry Pi with a camera for object recognition). Machine learning algorithms trained on images of waste materials allowed for a segregation accuracy rate of over 90%.

D. Dimensional Stability Assessment

After printing, specimens were measured using callipers and compared to their CAD models. Dimensional stability was tested under thermal cycling (20-60°C) and humidity (50-80% RH) for 48 hours. Warping and shrinkage were measured as percent changes in nominal dimensions.

RESULTS AND DISCUSSION

### A. Dimensional Accuracy

| Material | Shrinkage (%) | Warping (mm) | Tensile Strength (MPa) |
| --- | --- | --- | --- |
| Virgin PLA | 0.9 Â± 0.2 | 0.15 Â± 0.05 | 45.2 Â± 2.1 |
| Recycled rPET | 1.5 Â± 0.3 | 0.22 Â± 0.07 | 43.1 Â± 1.8 |
| rPET + Additives | 1.1 Â± 0.2 | 0.18 Â± 0.06 | 44.5 Â± 2.0 |

Recycled rPET specimens showed average shrinkage of 1.2-1.8%, compared to 0.8-1.2% for virgin PLA. Optimization reduced deviation to <1% by adjusting print speed. Table I summarizes key metrics.

### B. Integration in Waste Systems

Printed components were assembled into a prototype smart bin, achieving 95% segregation accuracy for plastics, metals, and glass. AI reduced processing time by 40% compared to manual sorting.

C. Sustainability Impact

Using recycled materials reduced CO2 emissions by 50-70% per part. Closed-loop recycling of print fails further minimized waste. Challenges include thermal degradation in recycled filaments, mitigated by blending with virgin materials.

CONCLUSION

This paper confirms that the components created using FDM printing, made from recycled waste, have sufficient dimensional stability for application in intelligent waste segregation systems. These systems, incorporating AI technology, will be able to work in a more efficient manner while also encouraging sustainability. In the future, there is a need to explore the applications of multi-material 3D printing.

REFERRENCE

[1] E. Zaneldin et al., "Dimensional Stability of 3D Printed Objects Made from Plastic Waste Using FDM: Potential Construction Applications," Buildings, vol. 11, no. 11, p. 516, 2021.

[2] M. Hassan et al., "3D printing in upcycling plastic and biomass waste to sustainable polymer blends and composites: A review," Mater. Des., vol. 230, p. 112019, 2024.

[3] C. Maraveas et al., "Evaluation of the Viability of 3D Printing in Recycling Polymers," Polymers, vol. 16, no. 8, p. 1104, 2024.